## Slide 1
Shai Carmi Bar-Ilan, BU
Together with: Shlomo Havlin, Chaoming Song, Kun Wang, and Hernan Makse

## Slide 2: Supercooled liquids
A liquid can be cooled fast enough to avoid crystallization, even below the freezing point.
At the glass transition temperature Tg, the liquid deviates from equilibrium, freezes in a meta-stable state, and becomes a glass.
The glassy state is disordered.
Tg depends on the cooling rate.

## Slide 3: Glass concepts
Tg arbitrarily defined when the viscosity reaches 1013 P.
Glass=relaxation time is longer than the time of the experiment.
Strong and fragile glasses.
VTF equation:
Mode coupling theory equation:

## Slide 4: Relaxation
Cage effect
Stretched exponential

## Slide 5: Entropy crisis
Kauzmann temperature TK <Tg
Glass transition intervenes to avoid crisis, the system is frozen in the ideal glass state.
The crystal has zero entropy.
If the entropy of the supercooled liquid will be less than the crystal, the third law would be violated.

## Slide 6: Energy landscape
A 3N-dimensional hyper surface of potential energy in which the system’s state is moving.

## Slide 7: Energy landscape’s network
Molecular dynamics of Lennard-Jones clusters with one (MLJ) or two (BLJ) species to calculate basins and transition states.
Each basin is a node.
Basins separated by a first order saddle point are connected by a link.
Node size degree

## Slide 8: The network’s properties
The network is highly heterogeneous.
The degree is correlated with potential energy of the basins and the barrier heights.
Normal distribution of basins’ potential energies
Exponential distribution of energy barriers
The network is scale-free
Potential energy decreases with degree
Energy barriers grow with degree
Network remains connected in low energies

## Slide 9: Model for the dynamics
Why do we need a model?
Near the transition, typical time diverges so MD simulations are too slow.
Energy landscape is 3N-dimensional- too detailed.
Neglect vibrational relaxations within the basins.
In low temperature, dynamics is dominated by activated hopping between basins.
Number of nodes
Arrhenius law:
i
j
ΔEi,j
ΔEj,i
What is the model?

## Slide 10: Applications of the model
Different cooling rates
Infinitely slow cooling
Glass transition temperature
Relaxation time
Super-Arrhenius behavior- fragile glass
Correlation
Stretched exponential
Similar results for BLJ!

## Slide 11: Percolation theory of networks
Remove a random fraction of the links/nodes.
When does the network breaks down?
At criticality, largest cluster vanishes and second largest diverges.

## Slide 12: Application to the energy landscape
The probability of a link to be effective is
Remove ineffective links.
At TK, the connected part of the network vanishes.
The network is at the ideal glass state!
Numerical identification of TK for MLJ (0.26) and BLJ (0.47).
TK

## Slide 13: Toy model
Assumptions:
Solution:
If x<1: <τ>=∞
If x>1: <τ><∞
rate to leave / time to stay at node i
If ε<1: x increases with k—
<τ>=∞ for small degree nodes
If ε>1: x decreases with k—
<τ>=∞ for hubs
Network is scale-free

## Slide 14: Percolation in the model
ε<1
ε>1
Nodes with <τ>=∞ are traps and are removed from the network.
As temperature is lowered, more nodes are removed until the percolation threshold is reached → glass transition.
random failure
targeted attack
TC
γ
Use percolation theory:

## Slide 15: Summary
Glasses are abundant in nature and technology, but out of equilibrium so hard to understand.
Molecular dynamics and energy landscape representation simplify the problem.
Network theory suggests a model that captures the essential properties of the glass transition.
Enables access to low temperatures.
Percolation picture describes landscape near the transition.
Can be generalized and extended to make predictions.